## Slide 1
Substrate Dependence and Tunneling Operation of MoS2 Nanotransistors
Arthur Bowman III, Zhixian Zhou
Nanofabrication and Electron Transport Laboratory
Department of Physics and Astronomy

## Slide 2
Overview
Motivation
Device Fabrication
Results
Conclusions

## Slide 3
Motivation
n+
n+
P-type Substrate
L
Channel Region
Source Electrode
Drain Electrode
Gate Electrode
Channel
Oxide Layer
Metal Oxide Field Effect Transistors (MOSFETs):
Source → Gate → Channel → Drain
At the Nanoscale:
Electrostatic effects
Quantum Mechanical effects
Understanding them →
Next-generation biosensors
Sarkar et al, ACS Nano (2014)

## Slide 4
Motivation
Transitional metal
Mo, W, Ti
(d-block elements)
Chalcogen
S, Se, Te
(Oxygen group)
MX2
e.g. MoS2, MoSe2 , WS2, WSe2 etc.
Atomically thin, 2 Dimensional Channel Materials
→ Transition Metal Dichalcogenides (TMD)
Chemically stable, flexible and super strong with a reasonable band gap!
Hexagonal Layer Structure

## Slide 5: `
How do we measure TMD FET performance?
Carrier Mobility
Scattering Mechanisms that limit µ:
Optical phonons
Acoustic phonons
Charged impurities at substrate/dielectric interface
Surface “traps” due to roughness
Channel defects
→ Achieve high µ with ultra smooth, high k dielectric substrate
Motivation
Intrinsic
Extrinsic
1
e-
MoS2
Kis et al. reported µ ~ 60 cm2V-1s-1 at 240 K with high–k dielectric for monolayer MoS2.
(Nature Materials 2013)

## Slide 6
Motivation
OTMS SAM treated SiO2
Al2O3 on Si/SiO2
h-BN
Atomic Layer Depostion ~60 nm
Higher dielectric constant compared to SiO2
Higher excitation energy of optical phonons
High dielectric constant
Ultra Smooth Surface
Impurity free
2D layer structure similar to TMD
Si/SiO2 substrates
modified with
OTMS SAMto create a
hydrophobic surface
~290 nm clean SiO2
Which Substrates Should We Study?
S
D

## Slide 7
Motivation
FET Operation through quantum tunneling
Not much supply voltage needed
→ Low Power Applications
P-doped Source
Source Fermi Level
Van Der Waals Gap
Van Der Waals Gap
MoS2
MoS2
Gate
Fermi Level
EC
EV
EG
Tunnel Field Effect Transistors (TFET)

## Slide 8
Motivation
Subthreshold Swing (SS)
Thermionic limit
→ Achieve High Performance
Subthermionic TFET with
Nb-doped WSe2 source, Novel Gates
Sarkar et al, Nature (2015)
How can we improve TFET Performance?

## Slide 9
Device Fabrication
n+
n+
P-type Si
Begin with commercial SiO2 on P Type Si Substrate
Mechanical Exfoliation of TMD
Transfer onto Substrate
Electron Beam Lithography
Metal Deposition
Liftoff
Transfer stage
SiO2

## Slide 10
Results
On HBN
On SiO2

## Slide 11
Results
How do we know we’ve made
a good device?
Current Voltage Characteristics (I-V curves)
Ohmic contact on all substrates
HBN looks best

## Slide 12: `
Results
Field Effect Mobility
Corresponds to bulk material
I-V curve → Conductivity
→ Field effect mobility, geometric capacitance
h-BN looks best

## Slide 13
Results
Hall Effect Mobility
Corresponds to bulk + surface material
I-V curve → Hall coefficient
→ carrier density
→ (along with conductivity) Hall mobility
Agrees well with field effect mobility
on h-BN

## Slide 14
Results
MoS2 Channel
Thicknesses:
9 nm
5 nm
2 nm
MoS2
HBN
Nb-doped WSe2
Junction Area

## Slide 15
Results
Subthreshold Slope
TFET channel thickness 9 nm:
SS = 147 mv/decade
Channel thickness 2.3 nm:
SS = 110 mv/decade
Still above thermionic limit with HBN gate
9 nm
3 nm
Gate Dependence
How do we prove tunneling operation?

## Slide 16
Conclusions
Substrate Dependence
Optical-phonon scattering remains dominant below ~ 100 K on h-BN
On all other substrates extrinsic scattering mechanisms start to degrade the carrier mobility below ~ 200 K
The ultra-smoothness and high k environment of h-BN improves mobility
IN THE FUTURE: PHASE-ENGINEERED DIELECTRICS
Tunneling Operation
Subthreshold Swing of 0.05 % Nb-doped WSe2/ MoS2/h-BN devices were still above thermionic limit of 60 mv/decade
This could be due to intrinsic limitations of h-BN gates or non ideal fabrication
More h-BN gated devices, experiments with other gate materials needed
IN THE FUTURE: IONIC LIQUID GATING, BV DOPING

## Slide 17
Acknowledgements
The authors would like to acknowledge:
Nanofabrication and Electron Transport Labortatory Senior Students:
Hsun Jen Chuang, Bhim P. Chamlagain, Meeghage M. Perera
Wayne State Universtiy nFab core facility staff:
William Funk, Dan Durisin
Initiative for Maximizing Student Development (IMSD) Program
National Institute of Health
For making this research possible