## Slide 1: Intrinsic Transport Properties & Scattering Mechanisms in TMDs
Kraig Andrews
Nanofabrication & Electron Transport Laboratory
Dept. of Physics & Astronomy

## Slide 2
Motivation
Introduction
Device Fabrication
Preliminary Results
Future Work & Conclusion
Overview

## Slide 3
Graphene
High mobility
  104 cm2V-1s-1 at Troom1
  Upper limit 105 cm2V-1s-1 at Troom2
High Young’s Modulus
No Bandgap3
  Low Ion/Ioff ratio
Notes: Upper limit is for suspended graphene (i.e. removed substrate)

## Slide 4
TMDs
Transition Metal Dichalcogenides (TMDs)
Transition Metal Chalcogen
Mo, W, V S, Se, Te
MX2
(MoS2, MoSe2, WSe2, WS2)
Unique Band structure3
Extremely Strong
High Ion/Ioff ratio > 106
Notes: Band structure for (a) bulk MoS2, (b) four-layer MoS2, (c) bi-layer MoS2, and (d) Monolayer MoS2. Shows transition from indirect bandgap to direct bandgap. Arrows indicate the lowest energy transitions.

## Slide 5
Field Effect Transistors (FETs)
Si/SiO2 substrate
TMD channel
Ti/Au electrodes
  Source Channel Drain

## Slide 6
AFM
Optical
Device Characterization

## Slide 7
Contact Resistance
  Schottky barrier & mobility
Scattering mechanisms
  Understand impact on mobility
Study p-WSe2 doping effects
  Impurities & mobility degradation
Performance limits
  Device applications
Challenges

## Slide 8
How to measure FET performance?
Mobility μ
Mobility & Scattering
μ limited by scattering:
Optical phonons
Acoustic phonons
Interface scattering
Impurities/channel defects
Intrinsic
Extrinsic
Study these mechanisms & how they effect device performance

## Slide 9
Field-Effect Mobility μFE
Two-probe Rcontact exists
Four-probe Rcontact eliminated

## Slide 10
Hall Mobility μH
Determine carrier density directly
μRT ~ 102 cm2V-1s-1
μLow-T ~ 104 cm2V-1s-1

## Slide 11
High Temperature (~ 295K-100K)
  Phonon scattering dominated
  T , μ
Low Temperature (< 100 K)
  Diminished phonon scattering
  Extrinsic scattering dominated
  Coulomb, impurity, interface, defects
  T , μ
Temperature Dependence of μ

## Slide 12
Low contact resistance μ increased
Schottky barrier (SB)
  Fermi level mismatch at metal/semiconductor interface
How to reduce SB height and width
  Metal work functions
  Graphene contact interface
Contacts/SB

## Slide 13
Approach
  2D/2D Contacts
  Lowering SBH
  Doping
    Lightly (~0.01-0.05%)
    Degenerately (>0.5%)
Contact Resistance
0.05% Nb doped WSe2

## Slide 14
Fabrication

## Slide 15
Results
Notes: Contact Resistances for 0.05% Nb doped WSe2 at room temp (Rc = 2.35 kΩ μm), 0.5% Nb doped WSe2 at room temp (Rc = 0.195 kΩ μm) and at 5K (Rc = 0.185 kΩ μm).

## Slide 16
Mobility μH

## Slide 17
Mobility μFE

## Slide 18
Quantum Transport
Integer Quantum Hall Effect (IQHE) & Shubnikov-de Haas (SdH) oscillations
  Low Temperature (< 4K)
  High Magnetic Field (~10 T)
  High µ at Low T Required

## Slide 19
SdH & IQHE in MoS2
  τq-MoS2-1L = 0.18 ps5
  τq-BP-10nm = 0.12 ps6
Device quality
Cyclotron effective m
  melectrons, mholes

## Slide 20
Performance Limits
Theoretical 1L mobility at T=295K7
  ~320-410 cm2V-1s-1
Experimental mobility at T=295K8
  ~200 cm2V-1s-1
Ion/Ioff > 107, Ion ~ 300 μA/μm
How to close theoretical/experiment gap

## Slide 21
Summary
2D/2D contact strategy to lower Rcontact
Improve μ through hBN encapsulation
Determine quantum properties using low T and high B environment
Room T performance limits

## Slide 22
Acknowledgements
The authors would like to acknowledge:
Nanofabrication and Electron Transport Laboratory students:
  Hsun Jen Chuang, Bhim Chamlagain, Meeghage Madusanka Perera, Arthur Bowman III, Upendra Rijal, and Sagar Paudel
Committee Members: Dr. Zhixian Zhou,
Dr. Jian Huang, Dr. Ashis Mukhopadhyay, Dr. Mark Cheng

## Slide 23
Mobility and scattering mechanism

## Slide 24
Field-effect transistor
Device characteristics
Field-effect mobility
Hall mobility
Temperature dependence of mobility

## Slide 25
Contacts
Schotttky barrier