## Slide 1
Phase Engineered Atomically thin high-K
Dielectrics for 2D Electronics
Wayne State University
Physics & Astronomy
Sagar Paudel

## Slide 2
Introduction:
First Transistor 1947
Size of transistor decreased from 10 µm in 1970’s to submicron level nowadays
Development of Silicon based devices took the central focus
Two dimensional materials like Graphene attracted lot of interest
First Transistor
used computer 1953
Michigan Micro
Mote (M^3)
2015

## Slide 3
Graphene
Strong in-plane bond and weak inter-layer force
Uniform surface
Free from Dangling bonds
Stable at room temp
High Mobility
106cm2v-1s-1 at 2K
105 cm2 v-1s-1 room temp
Elac D.C.(2011)
Zero band gap
Notes: Applications of 2D : FETs, Optoelectronic devices, Topological insulators, electrocatalysts.
Landau (1937) and Peierls (1935) argued that strictly 2D crystals were
thermodynamically unstable and could not exist.

## Slide 4
Graphene like material with finite band gap
Thermally stable
Compatible
Excellent on-off ratio > 106
Graphene Like 2D material :
Transitional Metal Dichalcogenides
(TMD)

## Slide 5
MoS2 FET
Field effect mobility of MoS2 (8-40 nm) is found in tens of cm2 /Vs and on-off ratio higher than 105 .
Anthony Ayari et al., (2007)
The mobility for the single layer MoS2 FET on SiO2 is found in the range 0.1 – 10 cm2/Vs.
B. Radisavljevic et. al.,(2011)
The mobility of bi-layer MoS2 FET were extracted 10-15 cm2/Vs.
Han Wang et. al., (2012)
Room temperature mobility 50-200 cm2/Vs for bulk MoS2.
R. Fivaz et.al., (1967)

## Slide 6
Contact
Interface
High K dielectric integration
Challenges of MoS2 FET
In our study, we will be focusing on High K dielectric integration of MoS2 FET.

## Slide 7
Why High K dielectric ?
Electrostatic control of channel is achieved through the capacitive coupling between the gate and the channel region
Scaling requires reduction in the source and drain depth by the same scaling factor as gate length, to ensure the effective control of channel.
Decreasing the thickness of gate oxide provides same result as thickness is inversely proportional to C.
Metal
Oxide
Semi-conductor
Imaginary
capacitor
plate

## Slide 8
But ,
Finding new dielectrics having high dielectric constant !!
Replacing SiO2 by dielectric having high dielectric constant increases the capacitive coupling
Decreasing the gate oxide thickness gives rise to short channel effects:
  Increase in leakage current
  Reduction In On-off ratio
  Break down of gate oxide
Another Way,

## Slide 9
Criteria Required
Good thermal stability
Low density of intrinsic defects
Sufficient gate dielectric lifetime
Sufficient energy band-gap

## Slide 10
Source :Wu, M. et. Al., 2008
Possible Candidates

## Slide 11
AFM image of HfO2 on MoS2 surface by ALD
XPS image showing island type of growth
Source : Stephen M. et. al., (2013)
AFM image of Al2O3 deposited
by 30 ALD cycles on MoS2 .
Source: Azcati A et.al., 2014
They require complex growth process
Non-uniform deposition
Surface contamination
Needs Surface treatment
Problem in High K dielectric integration of TMD

## Slide 12
Solution
Two dimensional atomically flat high K dielectric obtained through mechanical exfoliation
Exfoliation of TaS2
substrate
Thermal Oxidation
300̊ C
3 hours

## Slide 13
XPS Study of Oxidized TaS2 :
Source : Kuo Y., 1992
26.7 eV
28.6 eV
Area ratio = 1.4
The energy position of these peaks is close to the binding energy of Ta in stoichiometric Ta2O5.

## Slide 14
TEM Study
MoS2
Oxidized TaS2

## Slide 15
AFM Study :
Before heating
After heating

## Slide 16
C-V Measurement :
Notes: Thickness of sample 18nm

## Slide 17
K = 12.6
Using
We found:
C-V Measurement (cont.) :

## Slide 18
Experimental Details :
1. Graphene Transfer
2. TaS2 Transfer
3. Oxidation
4. MoS2 Transfer
6. Gold Deposition
5. E-beam Lithography
Si-substrate
Graphene
Ta2O5
MoS2
Electrodes

## Slide 19
Platinum back-gate device :
Platinum
Ta2O5
MoS2

## Slide 20
AFM Characterization :
Graphene back gate device
Platinum back gate device
MoS2
Ta2O5
Grap
hene
Gold Electrode
Platinum
Ta2O5
MoS2
Gold Electrode
Pt = 22 nm
Ta2O5 = 12 nm
MoS2 = 6 nm
Gr : 8 nm
Ta2O5 : 18 nm
MoS2 : 7 nm

## Slide 21
Electrical Characterization
Output Characteristics
Graphene Back gate Device

## Slide 22
Transfer Characteristic
a
b
Linear plot
Semi-log plot

## Slide 23
Sub-threshold swing = ∆x / ( Order of ∆y )
70 mV/decade ~ SS
Sub-threshold Swing

## Slide 24
Mobility Calculation
µ ~ 55 cm2V-1s-1
Notes: Length = 4.05 um
Width = 3.62 um

## Slide 25
Hysteresis Behavior
Linear plot
Semi-log plot

## Slide 26
Platinum Back gate device
Output Characteristic
Transfer Characteristic
100 mV/decade < SS
µ ~ 50 cm2V-1s-1

## Slide 27
Future Works
Ta2O5 as Top Gate dielectric
Optimizing the Contacts with Graphene electrodes
Optimizing the thermal oxidation Process
Scaling of Dielectric thickness
Scaling of Channel length

## Slide 28
Acknowledgements
Advisor : Dr. Zhixian Zhou
Committee Members :
        Dr. Boris Nadgorny
        Dr. Ashis Mukhopadhyay
        Dr. Mark Ming-Cheng Cheng
Bhim Chamlagain, Quingsong Cui, Hsun Jen Chuang 'Ben',
Meeghage Perera.
Upendra, Kraig, Arthur, Prakash.

## Slide 29
THANK YOU.

## Slide 30
High K Dielectrics
thigh K = 10 nm
Ԑr, SiO2 = 3.9
Ԑr, Ta2O5 = 20
teq = 1.95 nm

## Slide 31
AFM Characterization :
MoS2
Ta2O5
Graphene
Gold Electrode
Graphene Back gate device
Platinum Back gate device
Platinum
Ta2O5
MoS2
Gold Electrodes

## Slide 32
Before heating
After heating
AFM Study :