## Slide 1: Intrinsic Transport Properties & Scattering Mechanisms in TMDs
Kraig Andrews
Dr. Zhixian Zhou
Nanofabrication & Electron Transport Laboratory
Dept. of Physics & Astronomy

## Slide 2
Motivation
Introduction
Device Fabrication
Preliminary Results
Future Work & Conclusion
Overview

## Slide 3
Graphene
High mobility
  104 cm2V-1s-1 at Troom1
  Upper limit 105 cm2V-1s-1 at Troom2
High Young’s Modulus
No Bandgap3
  Low Ion/Ioff ratio
Notes: Upper limit is for suspended graphene (i.e. removed substrate)

## Slide 4
TMDs
Transition Metal Dichalcogenides (TMDs)
Transition Metal Chalcogen
Mo, W, V S, Se, Te
MX2
(MoS2, MoSe2, WSe2, WS2)
Unique Band structure3
Extremely Strong
High Ion/Ioff ratio > 106
Notes: Band structure for (a) bulk MoS2, (b) four-layer MoS2, (c) bi-layer MoS2, and (d) Monolayer MoS2. Shows transition from indirect bandgap to direct bandgap. Arrows indicate the lowest energy transitions.

## Slide 5
Contact Resistance
Study p-WSe2 doping effects
Quantum transport properties
Performance limits
Challenges

## Slide 6
Approach
  2D/2D Contacts
  Lowering SBH
  Doping
Contact Resistance
0.05% Nb doped WSe2

## Slide 7
Results
Notes: Contact Resistances for 0.05% Nb doped WSe2 at room temp (Rc = 2.35 kΩ μm), 0.5% Nb doped WSe2 at room temp (Rc = 0.195 kΩ μm) and at 5K (Rc = 0.185 kΩ μm).

## Slide 8
Mobility

## Slide 9
Mobility

## Slide 10
Quantum Transport
Integer Quantum Hall Effect (IQHE) & Shubnikov-de Haas (SdH) oscillations
  Low Temperature (< 4K)
  High Magnetic Field (~10 T)
  High µ at Low T Required

## Slide 11
IQHE
Notes: Integer quantum hall effect in an Indium gallium arsenide (InGaAs) heterostructure.

## Slide 12
SdH & IQHE in MoS2

## Slide 13
SdH Oscillations
Cyclotron mass of electrons and holes
Carrier lifetimes
  τq = 0.18 ps in 1L MoS25 & τq = 0.12 ps in ~10 nm BP6
A
Notes: Cyclotron mass is the mass of electrons/holes at the Fermi level.

## Slide 14
Performance Limits
Theoretical 1L mobility at T=295K7
  ~320-410 cm2V-1s-1
Experimental mobility at T=295K8
  ~200 cm2V-1s-1
Ion/Ioff > 107, Ion ~ 300 μA/μm
How to close theoretical/experiment gap

## Slide 15
Summary
2D/2D contact strategy to lower Rcontact
Improve μ through hBN encapsulation
Determine quantum properties using low T and high B environment
Room T performance limits

## Slide 16
Acknowledgements
The authors would like to acknowledge:
Nanofabrication and Electron Transport Laboratory students:
  Hsun Jen Chuang, Bhim Chamlagain, Meeghage Madusanka Perera, Arthur Bowman III, Upendra Rijal, and Sagar Paudel
Committee Members: Dr. Zhixian Zhou,
Dr. Jian Huang, Dr. Ashis Mukhopadhyay, Dr. Mark Cheng